PUFFIN BASECOAT STUCOAT WASH RUST SERIES

One component synthesis acrylic coating. This product This product is stucoat wash with RUST  patern series application system consist of primer .base coat and top coat ,can be apply  on  concrete ,mdf ,gypsum ,and other substrate , Very suitable for coffee shops, restaurants and other buildings that want walls and ceilings or other areas to be unique and attractive

Properties

| COLOR | Bronze ,copper ,goldmetalic colour |
| --- | --- |
| GLOSSLEVEL | Satin 45-65) |
| FILMTHICKNESS,DRY(μm) | 20-30 |
| FILMTHICKNESS,WET(μm) | 60-100 |
| THEORETICALSPREADINGRATE(M²/L) | 6-8m2 |
| SOLIDS(VOL%) | 30±2 |
| DENSITY(g/cm3) | 0.92 |
| FLASHPOINT | 32ºC±2% |
| PRACTICALCOVERAGE | ALLOWAPPROPRIATELOSSFACTORS |

- Characteristics

  - Recommended	concrete ,mdf ,gypsum ,and other

substrate

- Usage

  - Surfacepreparation:	For lasting adhesion tot he

Subsequent product,all surfaces must be clean, dry and free from any contamination. Oil or grease should be removed.

  - Substrate MinimumR ecommended:	The surface should be assessed and

Treated in accordance with Substrate

minimum recommended for concrete: Min

Age of concrete 1 months with PH<9,

Moisture

content<17%.Clean,dryandfreefrom any

contamination

Coated substrate:	Clean, dry, free for any contamination sand undamaged compatibility coatings

  - Application:	Wash sytem

  - Dilution:	Thinner hg

  - Drying and Curing time:	Dryingandcuringtimesaredetermined under controlled temperatures and relative humidity below 85 %, and at average of the DFT range for the product

Walk-on-dry:	Minimumtimebeforethecoatingcan tolerate normal foot traffic without permanent marks, imprints or other physical damage.

Dry to over coat, minimum:	Theshortesttimeallowedbeforethe next coat can be applied

Surface (touch) Dry:	Thestateofdryingwhenslightpressure with a finger does not leave an imprint or reveal tackiness.

| SUBTRATETEMPERATURE(oC) | 5 | 10 | 23 | 40 |
| --- | --- | --- | --- | --- |
| SURFACEDRY(hours) | 10 | 6 | 3 | 1 |
| DRYONWALK(hours) | 20 | 10 | 5 | 3 |
| Drytoovercoat,minimum (hours) | 12 | 6 | 3 | 1 |

| 6)Heat resistance Temperature | Continuous | Peak |
| --- | --- | --- |
| Dry atmospheric Peaktemperaturedurationmax.1hour. | 120’C | 140’C |

The temperatures	listedrelatetoretentionofprotective properties. Aesthetic properties may suffer at these temperatures.

7) Product compatibility :	Dependingontheactualexposureofthe coating system, various primers and topcoats can be used in combination with this product.

- Precaution

  - Ensuretocleanthesurfacebeforeapplication.

  - Healthandsafety:

Pleaseobservetheprecautionarynoticesdisplayedonthe container.

Use under well ventilated conditions. Do not inhale spray mist. Avoid skin contact. Spillageontheskinshouldimmediatelyberemovedwithsuitablecleanser,soapand water. Eyes should be well flushed with water and medical attention sought immediately.

  - Storage :

The product must be stored in accordance with national regulations. Keep the containers in a dry, cool, well ventilated space and away from sources of heat and ignition.Containersmustbekepttightlyclosed.Handlewithcare.Shelflifeat23°C: 48Month(s)

- Packing:	7,5L set & 20L set