PUFFIN PRIMER STUCOAT WOODS

Is environment friendly modified  acrylic primer paint. This product can resist alkali and moisture and also brings good adhesion between topcoat and substrate for Puffin stucoat wash wood series and rust series ,wood mapple series ,wood graining series application system.

Features

- Water based

- Low VOC

- Formaldehyde Free

- Heavy Metal Free

- APEO Free

- Carbendazim free

- Excellent adhesion in extreme area

- Low odor

- Alkali, chalk and water resistant

- Environment friendly

Recommended use	Use as foundation layer for Puffin Stucoat wash woodstain series

And rust mix series coatings system

| Film thickness and spreading rate | Min | Max | Typical |
| --- | --- | --- | --- |
| Film thickness, dry (um) | 25 | 30 | 28 |
| Film thickness, wet (um) | 59 | 83 | 71 |
| Theoretical spreading rate | 16.9 | 12 | 14.1 |
| (m2/ l) |  |  |  |

| Physical properties Color | Transparent brown |
| --- | --- |
| Solids (Vol %)* | 42+/-2 |
| Flash point | Nonflammable |

Water resistant	Very good

Sanding properties	Excellent

*Measured according to ISO 3222:1998(E)

Performance Guide

| Gloss Level Indicator | Gloss |
| --- | --- |
| VOC Properties Weather | <60 g/L untinted Excellent when used as part of approved system |
| Heat Resistance | Softens at temperatures above 70°C |
| Water Resistance | Excellent when topcat with approved top coat paint. |
| Abrasion Resistance | Good when top coat |
| Solvent Resistance | Sensitive to aromatic hydrocarbons, alcohols and ketones. |

Application methods

Roller	Recommended

Brush	Recommended

Spray	Use airless spray or conventional spray

Application data

Mixing ratio (volume)	The paint is ready to use after proper stirring. If thinning is

required clean water may be added up to a maximum of 5 %

Guiding data airless spray

Pressure at nozzle	140-190 kg/cm2 (2100psi)

Nozzle tip	0.021”-0.027”

Spray angle	65’-80’

Filter	Check to ensure that filters are clean

Drying time	Drying time are generally related to air circulation, temperature, film thickness, and number of coats, and will be affected correspondingly.

The figures given in table are typical with:

- Good ventilation (outdoor exposure of free circulation of air)

- Typical film thickness

- One coat on top of inert substrate

- Relative humidity 70 %

| Substrate temperature | 10’C | 23’C | 40’C |
| --- | --- | --- | --- |
| Surface dry | 2h | 1 h | 0.5 h |
| Through dry | 8h | 6h | 4h |
| Dry to recoat minimum 1 | 4h | 2h | 1h |
| Dry to recoat minimum 2, 3 |  |  |  |

- Recommended data given for recoating with the same generic type of paint

- In case of multi coat application, drying time will be influenced by the number and sequence and by total thickness of previous coats applied-reference is made to corresponding system data sheet

- The surface should be dry and free from any contamination prior application of subsequent coat

The given data must be considered as guidelines only, the actual of drying time /time before recoating may be shorter or longer depending on film thickness, ventilation, humidity, underlying paint system, requirement for early handling and mechanical strength etc. A complete system can be described on a system sheet, where all parameter and special condition could be included.

Typical paint system	Exterior & interior

Puffin Primer wood	1 coat

Puffin Basecoat Stuccoat wash wood series 	1 coat(partial area)

Puffin Stuccoat wash wood series	1 coat

Puffin Stucco Clear Gloss / Doff	1 Coat

Other system may be specified depending on area of use

Surface Preparation	All surfaces must be thoroughly cleaned and free of all dirt, dust, grease, lose or flaking paint. Efflorescence or mold on masonry or concrete surfaces must be treated.

Occasionally an apparently sound old paint will lose adhesion when recoated, particularly if the new paint is darker in color. To avoid this, check the adhesion of the old paint by cutting an 'X' through a clean area of the film with a sharp blade, press cellulose tape firmly across the cut and rip if off. If the old paint comes off with the tape it should be removed before repainting.

Clean Up	Clean all equipment with water

Condition during application	Apply at a temperature between 10’C and 35’C, Temperature of substrate should be minimum 3’C above the dew point of the air, the temperature and relative humidity should be measured in vicinity of substrate

Storage	The product must be stored in tightly closed container and keep container in dry cold, well ventilation space, away from source of heat and ignition.

Handling	Handle with care, stir well before use

Packing size	1 Liters set ,5 liter set & 20 Liters set