# PT. Indowijaya Sakti Teguh

Jl. Pangeran Jayakarta 121/3-4, Jakarta Pusat www.puffinpaint.com Telp : 021- 62313238

=======================================================================

PUFFIN ART DECOARTIVE

is a 100% pure acrylic formulation with single and multicolout colour sands contain , this product has low PVC, high binder with specialty & optimal resin / latex, additive, surfactant, colorant and other green raw material. It is designed as motif coatings system with  the end surface can be coated other type coatings for get decorative artistic gold.copper ,bronze fluorescent and  other for get special motif end result

Features

- Water based with end surface artistic motif result

- 100% acrylic paint with outstanding performance resin / latex and selection colorant

- Low Voc

- Formaldehyde Free

- Heavy Metal Free

- APEO Free

- Carbendazim free

- Color durability

- Environment friendly

Recommended use	Motif coat for exterior/ interior suitable for new or painted

concrete masonry, plaster and brick work, gypsum and wood panel

| Film thickness and spreading rate | Minimum | Maximum | Typical |
| --- | --- | --- | --- |
| Film thickness, dry (um) | 2000 | 4000 | 3000 |
| Film thickness, wet (um) | 2200 | 44000 | 3000 |
| Theoretical spreading rate (m2/kg) | 0,25 | 0,5 | 0,35 |

Physical properties

Color	As per color card

Solids (vol %)*	80+/-2

Flash point	Nonflammable

*Measured according to ISO 3222:1998(E)

Application methods

Tools 			    Use	Steel raskam ,and other tools for made motif

Spray	Use hooper gun cement spray or conventional spray

Mixing ratio (volume)	The paint is ready to use after proper stirring if thinning is

required water may be added up to a maximum of 5%

Thinner/ cleaner	Water

Guiding data airless spray

Pressure at nozzle	140-190 kg/cm2 (2100psi) Nozzle tip	6”-8”

Spray angle	65’-80’

Filter	check to ensure that filters are clean

Drying time	Drying  time are generally related to air circulation, temperature,

film thickness, and number of coats, and will be affected correspondingly.

The figures given in table are typical with:

- Good ventilation ( outdoor exposure of free circulation of air )

- Typical film thickness

- One coat on top of inert substrate

- Relative humidity 70 %

| Substrate temperature | 10’C | 23’C | 40’C |
| --- | --- | --- | --- |
| Surface dry | 2h | 1 h | 0.5 h |
| Through dry | 8h | 6h | 4h |
| Dry to re coat minimum 1 Dry to re coat minimum 2, 3 | 4h | 2h | 1h |

- Recommended data given for re coating with the same generic type of paint

- In case of multi coat application, drying time will be influenced by the number and sequence and by total thickness of previous coats applied-reference is made to corresponding system data sheet

- The surface should be dry and free from any contamination prior application of subsequent coat

The given data must be considered as guidelines only, the actual of drying time /time before re coating may be shorter or longer depending on film thickness, ventilation, humidity, underlying paint system, requirement for early handling and mechanical strength etc, a complete system can be described on a system sheet, where all parameter and special condition could be included.

Typical paint system					Exterior

Puffin Primer Art Texture					1 coat

Puffin Art decorative 					1 coat

Puffin xtra gold,copper,silver and bronze or other paint 1-3 coat

Other system may be specified depending on area of use

Surface Preparation	All surfaces must be thoroughly cleaned and free of all dirt, dust, grease, loose or flaking paint. Efflorescence or mould on masonry or concrete surfaces must be treated.

Occasionally an apparently sound old paint will lose adhesion when recoated, particularly if the new paint is darker in color. To avoid this, check the adhesion of the old paint by cutting an 'X' through a clean area of the film with a sharp blade, press cellulose tape firmly across the cut and rip if off. If the old paint comes off with the tape it should be removed before repainting.

Clean Up	Clean all equipment with water

Condition during application	Apply at a temperature between 10’C and 35’C, Temperature of substrate should be minimum 3’C above the dew point of the air, the temperature and relative humidity should be measured in vicinity of substrate

Storage	The product must be stored in tightly closed container and keep container in dry cold, well ventilation space, away from source of heat and ignition.

Handling	Handle with care, stir well before use

Packing size	5 Kg & 20 Kg