# PT. Indowijaya Sakti Teguh

Jl. Pangeran Jayakarta 121/3-4, Jakarta Pusat www.puffinpaint.com Telp : 021- 62313238

=======================================================================

PUFFIN ART TEXTUROLL SINGLE COLOUR

is a 100% pure acrylic formulation with single colour smooth Single  colour sands texture designed for roll application metode , this product has It is designed for durability in extremely harsh tropical climate, 2x UV Protected Colors, outstanding protection against the destructive effects of UV rays and heat from Infrared(IR) rays, This product will not blister, flake or peel for 5 years ( minimum )

Features

- Water based with  end surface multi  colour texture smooth surface

- 100% acrylic paint with outstanding performance resin / latex and selection colorant

- Low Voc

- Formaldehyde Free

- Heavy Metal Free

- APEO Free

- Carbendazim free

- Excellent dirt pick up resistant

- Color durability

- 1 hour recoat and easy clean up

- Easy to apply by roll

- Environment friendl

Recommended use	Topcoat for exterior  interior suitable for new or painted interior

concrete masonry, plaster and brick work, gypsum and wood panel

| Film thickness and spreading rate | Minimum | Maximum | Typical |
| --- | --- | --- | --- |
| Film thickness, dry (um) | 700 | 1000 | 800 |
| Film thickness, wet (um) | 900 | 1150 | 1025 |
| Theoretical spreading rate (m2/kg) | 0,3 | 0,5 | 0,4 |

Physical properties

Color	As per color card

Solids (vol %)*	77+/-2

Flash point	Nonflammable

*Measured according to ISO 3222:1998(E)

Application methods

Roll 	Use roll tools metode

Mixing ratio (volume)	The paint is ready to use after proper stirring if thinning is

required water may be added up to a maximum of 5%

Thinner/ cleaner	Water

Drying time	Drying time are generally related to air circulation, temperature,

film thickness, and number of coats, and will be affected correspondingly.

The figures given in table are typical with:

- Good ventilation ( outdoor exposure of free circulation of air )

- Typical film thickness

- One coat on top of inert substrate

- Relative humidity 70 %

| Substrate temperature | 10’C | 23’C | 40’C |
| --- | --- | --- | --- |
| Surface dry | 2h | 1 h | 0.5 h |
| Through dry | 8h | 6h | 4h |
| Dry to re coat minimum 1 Dry to re coat minimum 2, 3 | 4h | 2h | 1h |

- Recommended data given for re coating with the same generic type of paint

- In case of multi coat application, drying time will be influenced by the number and sequence and by total thickness of previous coats applied-reference is made to corresponding system data sheet

- The surface should be dry and free from any contamination prior application of subsequent coat

The given data must be considered as guidelines only, the actual of drying time /time before re coating may be shorter or longer depending on film thickness, ventilation, humidity, underlying paint system, requirement for early handling and mechanical strength etc, a complete system can be described on a system sheet, where all parameter and special condition could be included.

Typical paint system	Exterior/Interior

Puffin Primer Art Texture	1 coat

Puffin Art Texturoll single colour 	1 coat

Puffin Art Clear Texture	1-3 coat Other system may be specified depending on area of use

Surface Preparation	All surfaces must be thoroughly cleaned and free of all dirt, dust, grease, loose or flaking paint. Efflorescence or mould on masonry or concrete surfaces must be treated.

Occasionally an apparently sound old paint will lose adhesion when recoated, particularly if the new paint is darker in color. To avoid this, check the adhesion of the old paint by cutting an 'X' through a clean area of the film with a sharp blade, press cellulose tape firmly across the cut and rip if off. If the old paint comes off with the tape it should be removed before repainting.

Clean Up	Clean all equipment with water

Condition during application	Apply at a temperature between 10’C and 35’C, Temperature of substrate should be minimum 3’C above the dew point of the air, the temperature and relative humidity should be measured in vicinity of substrate

Storage	The product must be stored in tightly closed container and keep container in dry cold, well ventilation space, away from source of heat and ignition.

Handling	Handle with care, stir well before use

Packing size	1 Kg & 5 Kg & 20 Kg