# PT. Indowijaya Sakti Teguh

Jl. Pangeran Jayakarta 121/3-4, Jakarta Pusat www.puffinpaint.com Telp : 021- 62313238

PUFFIN STUCOAT PERLATOE

is a low odour and environment friendly water base modified acrylic emulsion. This product is water base with pearlescent effect. Very luxury motif pattern.

# Features

- Water based

- Fast dry

- Low VOC

- Formaldehyde Free

- Heavy Metal Free

- APEO Free

- Carbendazim Free

- Low Odour

- Environment friendly

- Easy application by raskam and wash system

Recommended use	Use as material coatings  for stucoat perlatoe coating system

| Film thickness and spreading rate | Minimum | Maximum | Typical |
| --- | --- | --- | --- |
| Film thickness, dry (um) | 50 | 80 | 65 |
| Film thickness, wet (um) | 100 | 160 | 130 |
| Theoretical spreading rate (m2/ liter)/1 coat | 4 | 8 | 6 |

# Physical properties

Colour	colour chard

Solids (vol %)*	51+/-2

Flash point	Nonflammable

# Application methods

Raskam system	Recommended

Wash system	Recommended

# Application data

Mixing ratio (volume)	The paint is ready to use after proper stirring, if thinning is required water may be added up to a maximum of 5%

Thinner/ cleaner	Water

Drying time	Drying time are generally related to air circulation, temperature, film thickness, and number of coats, and will be affected correspondingly.

The figures given in table are typical with:

- Good ventilation (outdoor exposure of free circulation of air)

- Typical film thickness

- One coat on top of inert substrate

- Relative humidity 70 %

| Substrate temperature | 10’C | 23’C | 40’C |
| --- | --- | --- | --- |
| Surface dry | 1h | 0,5h | 0.25 h |
| Through dry | 4h | 3h | 2h |
| Dry to re coat minimum 1 | 2h | 1h | 0,5h |

Dry to rec oat minimum 2, 3

- Recommended data given for re coating with the same generic type of paint

- In case of multi coat application, drying time will be influenced by the number and sequence and by total thickness of previous coats applied-reference is made to corresponding system data sheet

- The surface should be dry and free from any contamination prior application of subsequent coat

The given data must be considered as guidelines only, the actual of drying time /time before re coating may be shorter or longer depending on film thickness, ventilation, humidity, underlying paint system, requirement for early handling and mechanical strength etc., acomplete system can be described on a system sheet , where all parameter and special condition could be included.

Typical paint system	Stuccoat Perlatoe Coating system

Other system may be specified depending on area of use

Surface Preparation		Wall surface must be thoroughly cleaned and free of all dirt, dust, grease, and already 30 days age

Clean Up	Clean all equipment with water

Condition during application	Apply at a temperature between 10’C and 35’C, Temperature of substrate should be minimum 3’C above the dew point of the air, the temperature and relative humidity should be measured in vicinity of substrate

Storage	The product must be stored in tightly closed container and keep container in dry cold, well ventilation space, away from source of heat and ignition.

Handling	Handle with care, stir well before use

Packing size	1L & 7,5 L & 20L set ( base coat and top coat)