PT. INDOWIJAYA SAKTI TEGUH

Jl. Pangeran Jayakarta No. 121/3–4, Jakarta Pusat 10730, Indonesia

www.puffinpaint.com  |  Tel.: +62 21 6231 3238

TECHNICAL DATA SHEET

PUFFIN EPOXY EVOLAC CLEAR MULTIFUNGSI

# 1. PRODUCT DESCRIPTION

A two-component, polyamine-cured, solvent-free epoxy Novolac coating designed for use as a topcoat or single-coat system. It offers chemical resistance for medium-to-high chemical exposure, abrasion resistance, and a hard surface for medium-to-heavy traffic areas. Suitable for interior wood, carbon steel, galvanised steel, stainless steel, aluminium, stone, and concrete, with an application thickness of 300–2,000 µm.

# 2. TYPICAL PROPERTIES

| Property | Value |
| --- | --- |
| Colour | Transparent clear |
| Gloss level | Gloss, 75–85 |
| Dry-film thickness | 300–2,000 µm |
| Wet-film thickness | 300–2,000 µm |
| Theoretical spreading rate | 3–0.5 m²/L |
| Solids by volume | 99% ± 2% |
| Density | 1 g/cm³ |
| Flash point | 18°C ± 2°C |
| Practical coverage | Allow for appropriate loss factors |

# 3. RECOMMENDED USE

Recommended as a single coat or topcoat for interior wood, carbon steel, galvanised steel, stainless steel, aluminium, stone, and concrete where chemical resistance, abrasion resistance, and a hard surface are required.

# 4. SURFACE PREPARATION

All surfaces must be clean, dry, and free from oil, grease, dust, and other contamination. Remove oil and grease using a suitable cleaning method before application.

| Substrate | Minimum recommended preparation |
| --- | --- |
| Carbon steel | Abrasive blast-clean to Sa 2½ (ISO 8501-1). |
| Concrete | Minimum concrete age: 1 month; pH < 9; moisture content < 17%. Surface must be clean, dry, and free from contamination. |
| Wood | Surface must be clean and dry. Remove contamination using detergent and fresh-water cleaning. |
| Stainless steel | Cleanliness and surface profile corresponding to Sa 2½, Fine G (ISO 8503-2). |
| Aluminium | Abrade by hand or machine using non-metallic abrasives or bonded-fibre pads to create a scratch pattern and remove polish. Dry abrasive blast-cleaning to SSPC-SP 13/NACE No. 6. |
| Galvanised steel | Surface must be clean, dry, rough, and dull. Light brush-blast using non-metallic abrasive to create an even profile. |
| Stone | Clean, dry, and free from contamination. |
| Previously coated surfaces | Clean, dry, free from contamination, and coated with an undamaged compatible coating (ISO 12944-4, 6.1). |

# 5. APPLICATION DATA

| Item | Information |
| --- | --- |
| Application methods | Trowel, airless spray, conventional spray, brush, or roller |
| Airless spray pressure | Minimum 150 bar / 2,100 psi |
| Nozzle tip | 0.013–0.019 inch |
| Filter | Check that filters are clean |
| Brush | Recommended for stripe coating and small areas |
| Important | Apply carefully to achieve the specified dry-film thickness. |

# 6. MIXING RATIO

| Component | Mixing ratio by source |
| --- | --- |
| Puffin Epoxy Clear Multifungsi Base A | 2 parts |
| Puffin Epoxy Clear Multifungsi Base B | 1 part |

# 7. DRYING AND CURING TIMES

Values are based on controlled temperatures, relative humidity below 85%, and the average specified dry-film thickness. “Walk-on dry” is the minimum time before normal foot traffic can occur without permanent marks. Minimum overcoating time is the shortest interval before applying the next coat.

| Substrate temperature | 5°C | 10°C | 15°C | 23°C | 40°C |
| --- | --- | --- | --- | --- | --- |
| Surface dry (hours) | 1 | 12 | 6 | 4 | 3 |
| Walk-on dry (hours) | 24 | 20 | 18 | 12 | 4 |
| Minimum overcoating time (hours) | 24 | 20 | 18 | 12 | 4 |
| Maximum overcoating time (hours) | 180 | 150 | 72 | 48 | 30 |
| Dry/cured for service (days) | 20 | 15 | 10 | 7 | 3 |

# 8. PRODUCT COMPATIBILITY

Compatible primer and topcoat selection depends on the actual exposure and coating system. Typical subsequent coats include epoxy and polyurethane coatings.

# 9. HEALTH, SAFETY, AND PRECAUTIONS

Clean the surface before application. Observe all precautionary notices on the container. Use in well-ventilated conditions. Do not inhale spray mist. Avoid skin and eye contact. Remove skin contamination immediately using a suitable cleanser, soap, and water. Flush eyes thoroughly with water and seek immediate medical attention. Refer to the applicable MSDS for complete safety information.

# 10. STORAGE AND PACKAGING

| Item | Information |
| --- | --- |
| Storage | Store in accordance with national regulations. Keep containers tightly closed in a dry, cool, well-ventilated area away from heat and ignition sources. Handle with care. |
| Shelf life | 24 months at 23°C |
| Pack sizes | 1.5 kg, 7.5 kg, and 20 kg per set |

## IMPORTANT NOTE

The technical values above reproduce the source document. Application conditions, substrate condition, and loss factors may affect actual performance and coverage. Verify critical project requirements before use.