PT. INDOWIJAYA SAKTI TEGUH

Jl. Pangeran Jayakarta No. 121/3–4, Jakarta Pusat 10730, Indonesia

www.puffinpaint.com  |  Tel.: +62 21 6231 3238

TECHNICAL DATA SHEET

PUFFIN AEROSILCOAT STOVE

A silicone acrylic with aliphatic-cured hybrid material for high-performance coatings, especially high-temperature and wear-resistant applications. Suitable for aluminium, steel, iron, stainless steel, and other substrates using a stoving system.

| Color | Catalog |
| --- | --- |
| Gloss Level | Glossy (80–95), Satin (40–70), Matt (20–30) |
| Film Thickness, Dry (µm) | 25–35 |
| Film Thickness, Wet (µm) | 50–75 |
| Theoretical Spreading Rate (m²/L/layer) | 10–12 |
| Solids (Vol. %) | 42 ± 2% |
| Density (kg/L) | 1 |
| Curing Time | 100–120°C / 30–60 minutes |
| Flash Point | 35°C |
| Practical Coverage | Allow appropriate loss factors |

# 1. Characteristics

Designed primarily for painting new substrates with a stoving system.

Recommended for properly prepared carbon steel, galvanized steel, stainless steel, and aluminium.

# 2. Usage

## Surface Preparation

To secure lasting adhesion to subsequent products, all surfaces shall be clean, dry, and free from contamination.

## Minimum Recommended Substrate Preparation

| Substrate | Recommended Preparation |
| --- | --- |
| Carbon Steel | Sa 2½ (ISO 8501-1) and iron phosphate pre-treatment. |
| Coated Surfaces | Clean, dry, and undamaged compatible coating. |
| Stainless Steel | Hand or machine abrade with non-metallic abrasives or bonded fibre abrasive pads to impart a scratch pattern. |
| Galvanized Steel | Surface shall be clean, dry, rough, and dull; use iron phosphate pre-treatment. |
| Aluminium | Dry abrasive blast cleaning to SSPC-SP 13/NACE No. 6 and use green/yellow chromate pre-treatment. |

## Application

| Application Method | Airless spray |
| --- | --- |
| Pressure at Nozzle (minimum) | 150 bar / 2,100 psi |
| Nozzle Tip (inch/1000) | 17–21 |
| Filter | Check to ensure filters are clean. |
| Mixing Ratio | Puffin Aerosilcoat Base A: 2 parts; Puffin Aerosilcoat Base B: 1 part |
| Thinning | Thinner PU |
| Drying and Curing Time | 30–60 minutes at 100–120°C |

## Product Compatibility

Depending on actual exposure of the coating system, various primers can be used in combination with this product. Previous coat: iron phosphate pre-treatment.

# Precautions

Ensure the surface is clean before application.

Observe precautionary notices displayed on the container. Use under well-ventilated conditions. Do not inhale spray mist. Avoid skin contact.

Spillage on skin should immediately be removed with suitable cleanser, soap, and water. Eyes should be flushed with water and medical attention sought immediately.

Store in accordance with national regulations. Keep containers in a dry, shaded, cool, well-ventilated space away from heat and ignition sources. Keep containers tightly closed and handle with care.

# Packing

1 / 5 / 20 Liter Set