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TECHNICAL DATA SHEET
PUFFIN AEROSILCOAT STOVE

A silicone acrylic with aliphatic-cured hybrid material for high-performance coatings, especially high-temperature and wear-resistant applications. Suitable for aluminium, steel, iron, stainless steel, and other substrates using a stoving system.
	Color
	Catalog

	Gloss Level
	Glossy (80–95), Satin (40–70), Matt (20–30)

	Film Thickness, Dry (µm)
	25–35

	Film Thickness, Wet (µm)
	50–75

	Theoretical Spreading Rate (m²/L/layer)
	10–12

	Solids (Vol. %)
	42 ± 2%

	Density (kg/L)
	1

	Curing Time
	100–120°C / 30–60 minutes

	Flash Point
	35°C

	Practical Coverage
	Allow appropriate loss factors


1. Characteristics
Designed primarily for painting new substrates with a stoving system.
Recommended for properly prepared carbon steel, galvanized steel, stainless steel, and aluminium.
2. Usage
Surface Preparation
To secure lasting adhesion to subsequent products, all surfaces shall be clean, dry, and free from contamination.
Minimum Recommended Substrate Preparation
	Substrate
	Recommended Preparation

	Carbon Steel
	Sa 2½ (ISO 8501-1) and iron phosphate pre-treatment.

	Coated Surfaces
	Clean, dry, and undamaged compatible coating.

	Stainless Steel
	Hand or machine abrade with non-metallic abrasives or bonded fibre abrasive pads to impart a scratch pattern.

	Galvanized Steel
	Surface shall be clean, dry, rough, and dull; use iron phosphate pre-treatment.

	Aluminium
	Dry abrasive blast cleaning to SSPC-SP 13/NACE No. 6 and use green/yellow chromate pre-treatment.


Application
	Application Method
	Airless spray

	Pressure at Nozzle (minimum)
	150 bar / 2,100 psi

	Nozzle Tip (inch/1000)
	17–21

	Filter
	Check to ensure filters are clean.

	Mixing Ratio
	Puffin Aerosilcoat Base A: 2 parts; Puffin Aerosilcoat Base B: 1 part

	Thinning
	Thinner PU

	Drying and Curing Time
	30–60 minutes at 100–120°C


Product Compatibility
Depending on actual exposure of the coating system, various primers can be used in combination with this product. Previous coat: iron phosphate pre-treatment.
Precautions
Ensure the surface is clean before application.
Observe precautionary notices displayed on the container. Use under well-ventilated conditions. Do not inhale spray mist. Avoid skin contact.
Spillage on skin should immediately be removed with suitable cleanser, soap, and water. Eyes should be flushed with water and medical attention sought immediately.
Store in accordance with national regulations. Keep containers in a dry, shaded, cool, well-ventilated space away from heat and ignition sources. Keep containers tightly closed and handle with care.
Packing
1 / 5 / 20 Liter Set
Puffin Aerosilcoat Stove TDS




